## Slide 1
AGENDA
8:15-8:30 |  | Self introductions
8:30-8:45 |  | David Shifler, Introductory remarks
8:45-9:30 |  | Martin Harmer, Overview of MURI project
9:30-11:45 |  | Presentations by individual MURI team members plus guest scientist, Alexis Lewis.
Note: Anthony Rollett from Carnegie Mellon University will be in Europe, but will participate remotely. |  | 
 | 9:30-9:45 | Andrea Harmer, Kutztown University
 | 9:45-10:00 | Helen Chan, Lehigh University
 | 10:00-10:15 | Jeffrey Rickman, Lehigh University
 | 10:15-10:30 | Michael Widom, Carnegie Mellon University
10:30-10:45 |  | Break
 | 10:45-11:00 | Jian Luo, Clemson University
 | 11:00-11:15 | Greg Rohrer, Carnegie Mellon University
 | 11:15-11:30 | Shen Dillon, University of Illinois
 | 11:30-11:45 | Alexis Lewis, Naval Research Laboratory
12:00-1:00 |  | Lunch and discussion, Tower Room, Mountaintop Campus
1:00-1:45 |  | Alan Pense, * Tour of ATLSS national earthquake testing laboratory and composite ship building laboratory, Mountaintop Campus.
1:45-2:15 |  | Private meeting for review team -ATLSS Conference Room B144
2:15-2:30 |  | Feedback and discussion
2:45-3:00 |  | Demonstration of Spark Plasma Sintering, 3rd floor Whitaker Lab
3:00-3:30 |  | Tour of Electron Microscopy Laboratory, 1st floor Whitaker Lab
3:30 |  | Depart
AGENDA

## Slide 2: Tailoring of Atomic-Scale Interphase Complexions for Mechanism-Informed Material Design
Martin P. Harmer
Office of Naval Research Multidisciplinary University Research Initiative Project
Kickoff Meeting, Thursday June 23rd 2011
ONR Topic Chief: David Shifler

## Slide 3: Outline
• Participants in MURI Program
• Introduction to Interphase Complexions (IC’s) Concept
• Examples of IC’s in Ceramic and Metal Systems
• Objectives and Goals of the MURI Program
• Thrust 1: Creation of New Classes of Materials with Tailored Properties
• Thrust 2: Exploitation of Complexions in the Processing of Bulk Nano- grain Materials
• Thrust 3: Exploitation of Complexions in Controlling Properties in Strategic Engineering Materials
• Management/Future Meetings
• Recruitment
• MURI-Related Affiliations

## Slide 4: Participating Institutions
Lehigh University
  Martin P. Harmer (PI), Helen M. Chan, Jeffrey M. Rickman, Ed Webb
Carnegie Mellon University
  Gregory S. Rohrer, Anthony D. Rollett, Michael Widom
Clemson University
  Jian Luo
University of Illinois Urbana-Champaign
  Shen J. Dillon
Kutztown University of Pennsylvania
  Andrea J. Harmer

## Slide 5
Complexion
Bulk B
Bulk A
Complexion
com·plex·ion noun \kəm-ˈplek-shən\
Atomic scale (0.2 – 2 nm) thermodynamically stable interface-stabilized phase (interphase) that does not exist in bulk form.
“The Phase Behavior of Interfaces”, Science, 332 [6026] 182-183 (8 April 2011).

## Slide 6: Complexions: Characteristics
Complexions are transformable like phases (crystallography, chemistry, temperature important).
Characteristic thickness with varying degree of disorder (6 distinct layering transitions) – new taxonomy.
Superimposable onto bulk phase diagrams – Complexion Diagrams.
Different complexions have vastly different kinetics and probably physical properties.
“Interfacial Kinetic Engineering: How Far Have We Come Since Kingery’s Inaugural Sosman Address?”,
J. Am. Ceram. Soc., 93 [2] 301–317 (2010)
Courtesy of Steve Garofalini

## Slide 7: Example - Intergranular Films (IGF)
TiO2
SiO2
2 nm
Hetero-Interfaces
(Kwon et. al, APL 1999)
NOT classical solid-state amorphization
Cu
b.c.t.-Ta
(metastable)
Cu-Ta
Vapor
(Luo & Chiang,
Annu. Rev. Mater. Res. 2008)
Free Surfaces
Si3N4
2 nm
Si3N4
SiC,
AlN,
SIALON,
Al2O3,
(Sr, Ba)TiO3,
ruthenate thick film resistors,
TiO2, ZrO2, YBCO,
Synroc, etc.
(all with additives)
No SiO2, (Wang & Chiang, J. Am. Cer. Soc. 1998)
ZnO
ZnO
Ceramic Grain Boundaries (GBs)
Equilibrium thickness
D. Clarke,
J. Am. Ceram. Soc. 1977
Widespread Existence of Similar IGFs:
Metal-Oxide Interface
(Kaplan et al,
Acta Mater. 2000)
Cu
Al2O3
2 nm
Surface
(Wettlaufer, PRL 1999)
GB & interface
(Wettlaufer et al., PRE 2005)
Ice + Impurities, e.g. NaCl
(Molecular Solids)
Ni-enriched film
2 nm
T< Teutectic
W
W
(Luo, et al., APL 2005)
SiO2-enriched film
Oxide-Oxide
Hetero-Interface
(Ackler & Chiang,
J. Am. Cer. Soc. 1997)
ZnO
Bi2O3-enriched
film (w/o SiO2)
T< Teutectic
Ice
Vapor,
Ice, or
Inert Wall
Quasi-Liquid
T< Teutectic
Metals
Kleebe et al, J. Am. Cer. Soc. 1993
SiO2-enriched film

## Slide 8: Schematic of Complexion Types
S.J. Dillon, M. Tang, W.C. Carter, M.P. Harmer, Acta Mater. 2007

## Slide 9: Complexions - High Resolution Electron Microscopy
S.J. Dillon, M. Tang, W.C. Carter, M.P. Harmer, Acta Mater. 2007
Submonolayer segregation
Intrinsic, “clean”
Bilayer segregation
True Wetting Film
Intergranular film
Trilayer segregation

## Slide 10: Transport Properties of Complexions (Alumina)
S.J. Dillon, M. Tang, W.C. Carter, M.P. Harmer, Acta Mater. 2007

## Slide 11: Copper Oxide Doped Titania-complexion Type III, Bilayer
HRTEM
HAADF-STEM (smoothed and deconvoluted)
0.4 nm
Courtesy of ShuaiLei Ma

## Slide 12: Copper Oxide Doped Titania-complexion Type IV, Trilayer
HRTEM
HAADF-STEM (smoothed and deconvoluted)
0.6 nm
Courtesy of ShuaiLei Ma

## Slide 13: GB Complexions In Metal Systems
VI. Wetting IGF
Cu-Bi1
Al-Ga2
W-Ni3
Mo-Ni4
2nm
2nm
Ni
1. G. Duscher et al. Nature Materials, 2004
2. W. Sigle et al. Applied Physics Letters, 2006
3. J. Luo et al. Applied Physics Letters, 2005
4. X. Shi et al. Applied Physics Letters, 2009
?
IV. Trilayer

## Slide 14: GB Complexions in Ni-Bi Alloys
1 nm
J. Luo, H. Cheng, K. Meshinchi Asl, C. J. Kiely, M. P. Harmer, submitted to Science

## Slide 15: Thermodynamic Modelling
Stability Condition
a
a
a
a
b
C. Bishop et al., Mat. Sci. Eng. A., 2006.
J. Luo, X. Shi, Appl. Phys. Lett., 2008.
No Atomistic/First Principles Calculations of IC’s and their transitions to date

## Slide 16: Selection Rules
Complexion formation favored by:
• High energy grain boundaries in the host
• Compositions near deep eutectics
• Systems that produce second phases with large interphase boundary energies
• Alloy systems with low solubility and high segregation
16
Surface
Crystal 2
Ψs
Crystal 1
d
β
2W

## Slide 17: Tailorable Properties - Examples
S.C. Carniglia, J. Am. Cer. Soc., 1972
Nakamura et al, Nature Materials (2003)
Phenomenon | Properties | Examples
Grain Growth | Atomic diffusivity, | Al2O3
Creep, Oxidation, Densification | Atomic Diffusivity, | Refractory Metals (W, Mo), Al2O3, Si3N4
Electrical Conduction | Conductivity, | Al2O3-Ti
Mechanical | Strength, Toughness | Al2O3, WC-Co
Phenomenon | Properties | Examples
Grain Growth |  | Al2O3
Creep, Oxidation, Densification |  | Refractory Metals (W, Mo), Al2O3, Si3N4
Electrical Conduction |  | Al2O3-Ti
Mechanical | Strength, Toughness | Al2O3, WC-Co

## Slide 18: WC - Co Complexion-Property Relationship?
J. Vicens et al, J. Mat. Sci., 1994
E. Breval et al, Mat. Sci. & Engg., 2005
Z. Z. Fang et al, Int. J. Refr. Met. & Hard Mat., 2009
V. Jayaram et al, J. Am. Cer. Soc., 1983

## Slide 19: Proposed Approach

## Slide 20: Creation of New Classes of Materials with Tailored Properties
THRUST 1: OBJECTIVES
• Establish a set of “Selection Rules” for metal-complexionized ceramics (MCC).
• Develop complexion phase diagrams for MCC.
• Correlate individual complexion types with each of their associated physical properties (thermo-mechanical, diffusivity).
• Develop Ashby-type property maps incorporating important grain size (nanoscale) effects.
• Correlate individual boundary effects with distributions in polycrystalline microstructures.
• Develop processing strategies for controlling polycrystalline grain structures (e.g. unimodal vs. multi-modal, nano grain size vs. micron grain size etc).

## Slide 21: Creation of New Classes of Materials with Tailored Properties
THRUST 1: TECHNICAL APPROCH
Characterization
HREM (structure, chemistry), ELNES (local bonding)
SPM - Conduction Mode (conductivity of individual IC’s)
Nano-indentation
GB character and energy distribution
Thermal Properties
SIMS, GB diffusivity
Bicrystals
Model Sandwich Structures
Nanophase MCCs
MCC material system: Alumina – (Cu, Cu-Ti, Ni)

## Slide 22
Creation of New Classes of Materials with Tailored Properties
THRUST 1: MODELLING
Developing Interatomic Potentials
-- Phase Stability
-- Segregation Energies
-- GB Energies
-- Diffusion Barriers
First-Principles Calculations
Atomic Level Modelling & Simulations
Ab-Initio
Monte Carlo, Molecular Dynamics
-- Transport Properties
-- Mechanical Behavior
Mesoscale Simulations
Potts Model, Phase-field Method
-- Abnormal Grain Growth
Interphase Thermodynamic Modelling
Phenomenological, Sharp-Interface Model
-- Compute Complexion Phase Diagrams

## Slide 23: Exploitation of Complexions in the Processing of Bulk Nano-grain Materials
THRUST 2
Determine the critical role of IC’s in the application of fabrication processes for producing bulk nano-grain materials.
Two Step Sintering
Spark Plasma Sintering

## Slide 24: Exploitation of Complexions in the Processing of Bulk Nano-grain Materials
THRUST 2
Material Systems for Thrust 2 | 
Model Systems: | Alumina – silica/yttria
New Materials: | Nano metal-complexionized ceramics
Challenging Conventional Materials: | WC-Co, YSZ

## Slide 25: Exploitation of Complexions in Controlling Properties in Strategic Engineering Materials
Embrittlement of Ni & Cu Alloys
THRUST 3
Ionic Conductivity of Oxides
Model System: ZrO2-Y2O3-(SiO2)-MxOy
Co-dope to control GB resistance
Synthesis of specimens
High-T impedance measurements
HRTEM, HAADF-STEM (Lehigh)…
Systematic Co-doping
Characterization
Other Systems
Sn and Sb doped ZnO
Al-B4C
····
Revisit WC-Co
Systematic investigation of grain boundary mobility and the formation and stability of complexion as a function of temperature chemistry
Develop interphase engineered nano MCC of WC-Co.

## Slide 26: Management
http:\\muri.cc.lehigh.edu
MURI Research Group Meetings
Monthly teleconference
Biyearly face to face meetings: December and Mid-June
Annual ONR Review Meeting
Bear Creek International Conference on Interfaces October 2-6, 2012
Reporting Requirements?

## Slide 27: US Student/PostDoc Recruitment
LEHIGH UNIVERSITY
Abigail Lawrence (US citizen), Michael Kracum (US citizen), Denise Yin (US citizen), Patrick Cantwell (US citizen), Suxing Wu (US citizen),
Animesh Kundu
CLEMSON UNIVERSITY
Yuanyao Zhang, Matthew Williams (US citizen)
CARNEGIE MELLON UNIVERSITY
Stephanie Bojarski (US citizen)
UNIVERSITY of ILLINOIS AT URBANA-CHAMPAIGN

## Slide 28: MURI-RELATED AFFILIATIONS
DOD PARTNERSHIPS
ARL
James Sands
Michael (Mick) Maher
Gary Gilde
ARO
David Stepp
Doug Kiserow
ARDEC Picatinny
John Theis
Stacey Kerwein
Chris Haines
AFOSR/WPAFB
Ali Sayir/Randall Hay
NRL
Alexis Lewis
POTENTIAL INDUSTRY PARTNERS
Material Complexions Inc.
TA&T
Thermal Technologies Inc
Dupont
GE