## Slide 1
Developing Thermodynamic Theories & Models
  Putting our models/efforts in a broader context of existing prior models
    Classical GB segregation models;
    GB “phase” transitions;
    Prewetting/premelting type models;
    Some of our prior efforts/models
  Predictive?
  Unified, big picture: how different models connect?
  Connect to atomistic/DFT?
Experimental Efforts
  Metallic Systems: Ni-Bi, Cu-Bi and Fe-Bi
  Ionics: YSZ and BZY
Office of Naval Research Multidisciplinary University Research Initiative Project
Pre-Review Meeting, May 17th 2011
ONR Topic Chief: David Shifler

## Slide 2
Ceramic
Metal
Complete Wetting
“Arbitrary” Thickness
“Moist”
(R.M. Cannon)
Prewetting and/or Premelting
“Equilibrium” Nano Thickness
Well-Known
Well-Known
Continuous h ~ nm
The Bigger Picture…
h  +
Discrete Thickness

## Slide 3: The Classical Grain Boundary (GB) Segregation (= Adsorption) Models
McLean-Langmuir Adsorption
Hondros-Seah (BET like multilayer adsorption)
Assuming that adsorbates are pure B
All developed via surface-GB analogies…
Lejcek-Hofmann (for non-ideal solutions); still fixed # of adsorption sites
Assume: both bulk & GB phases are ideal solution
Assuming GB as a separate “phase” in equilibrium with the bulk phase
“monolayer”? – in reality, not necessarily in the same layer

## Slide 4: Segregation Energy/Enthalpy
Surface Segregation (Wynblatt and Ku)
Elastic Energy
GB Core:
Fraction of broken bonds
“Regular-Solution Correction”
Inside:
GB Segregation (Wynblatt and Chatain)

## Slide 5: GB (Chemical) Phase Transition in the Classical Model
Fowler-Guggenheim (1939)

XC
1st order if
Intrinsic
(nominally “clean”)
“Monolayer”
Hart et al. (1960’s) used a similar model to explain tempering embrittlement.
Attractive adsorbate-adsorbate interactions  1-order interfacial “phase” transition…

## Slide 6: GB (Chemical) Phase Transition in the Classical Model

XC
1st order if
Intrinsic
(nominally “clean”)
“Monolayer”
Fowler-Guggenheim (1939)
Attractive adsorbate-adsorbate interactions  1-order interfacial “phase” transition…
van der Waals Equation
(Nobel Prize 1910)
Attractive molecule-molecule interactions  1st -order phase transition…

## Slide 7: GB (Chemical) Phase Transition in the Classical Model

XC
1st order if
Intrinsic
(nominally “clean”)
“Monolayer”
Fowler-Guggenheim (1939)
Attractive adsorbate-adsorbate interactions  1-order interfacial “phase” transition…
Regular Solutions
1-order “phase” transition if…

## Slide 8: The Ni-Bi and Si-Au Cases
Miedema = -14.8 kJ/mol
Au Bilayer
Si
Si
Miedema = -59.2 kJ/mol
Repulsive Adsorbate-Adsorbate Interactions
Strong A-B:
½|EA-A| + ½|EB-B| < |EA-B|
RNi = 1.35Å; RBi = 1.6Å;
|ENi-Ni| >> |EBi-Bi|
RSi = 1.1Å; RAu = 1.35Å;
|ESi-Si| > |EAu-Au|
Strong Segregation System

## Slide 9
Bilayer Structure
 Embrittlement
Energetically
The Most Favored!
Strong Ni-Bi: ½|ENi-Ni| + ½|EBi-Bi| < |ENi-Bi|
Weak Bi-Bi: |EBi-Bi| << |ENi-Ni|
Verified by HAADF STEM
Each Bi layer coherently adsorbed on the adjacent Ni grain
Incoherent between the 2 Bi layers
Ni grain
Ni grain
Adsorbed Bi
Adsorbed Bi
Virtually no relaxation
Like a Bi-Bi GB?

## Slide 10
In collaboration with
Lehigh
Ma & Harmer
Ma et al.
Scripta Mater.
2012
discontinuity
in GB excess
“Clean”
Intrinsic GB
Au Bilayer
1st order GB “phase” transition
Si
Si
Si
Si
Si
Si
Strong Si-Au:
½|ESi-Si| + ½|EAu-Au| < |ESi-Au|
Miedema model

## Slide 11: Predictive Thermodynamic Model? To Some Extend!
Ni-Bi
Ni-Bi = -14.8 kJ/mol
Cu-Bi = +14.2 kJ/mol
Cu-Bi
Fe-Bi
Cu-Bi = +72.3 kJ/mol
Bilayers ubiquitous
Homologous Temperature Tanneal/Tmelt = 0.5637
A Designed Experiment
Tanneal = 700 C
Tanneal = 492 C
Tanneal = 746 C
Bilayers observed, but in a narrow window
Bilayer NOT observed

## Slide 12: Why no classical 1st order adsorption transition in Fe-Bi?
Fe-Bi
Cu-Bi = +72.3 kJ/mol

XC
1st order if
Intrinsic
(nominally “clean”)
“Monolayer”
1-order “phase” transition if…
Limited solubility of Bi in Fe
Zhiyang’s STEM  “Clean” GB

## Slide 13: A Sophisticated GB Segregation Model Wynblatt and Chatain [JMS 2005; 2006, MMA 2007]
GB Core:
Inside:
Segregation Enthalpy
Same Crystal Structure
A weak “bilayer” in Pt-Au
3 % Au
Weak Segregation Systems?

## Slide 14: A Solid-State GB Prewetting Transition Predicted
Wynblatt, Chatain, Mater. Sci. Eng. A 2008
Solid Miscibility Gap

## Slide 15: Background – for the Student Audience Prewetting & Multilayer Adsorption Cahn, J. Chem. Phys. 66: 3667 (1977)
Surface Excess
Critical-Point Wetting Model (Cahn)
De-mixed binary liquids
Binary Liquid
Multilayer Gas Adsorption
Multilayer Adsorption
“Strong” Substrate  Layering
Pandit, Schick, Wortis
Phys. Rev. B, 26, 5112 (1982)
TC
Tw
monolayer
bilayer
TR
 - 0
A
B
C
D
D
Mathematically Isomorphic

## Slide 16: Origin of 1st-Order Transition: A Generalized Cahn Model
dry
IGF
Binary (solid-liquid) eutectic systems
For GBs: Tang, Carter & Cannon, PRL 2006
For Surfaces: Luo, Tang, Cannon, Carter & Chiang, MSEA 2006
Prewetting & Critical-Point Wetting
for binary de-mixed liquids
Cahn, J. Chem. Phys. 66:3667 (1977)
f : vol. free energy
 : surface term
c : concentration
c : gradient (c) energy coefficient
Include additional field variables
 : crystallinity
 : orientation
 : gradient () energy coefficient
c
thin
thick
Cahn’s graphical construction
Quasi- surface phase

## Slide 17: A Further Elaboration (CalPhaD Data Used)
Mishin et al., Acta Mater. 2009
Cu-Ag
GB Energy vs. Interfacial Width
A Low-Energy GB
A High-Energy GB

## Slide 18
Crystalline Grain
Crystalline Grain
Crystal
Prewetting
-like layer

Cahn, "Critical Point Wetting," J. Chem. Phys. 66, 3667 (1977)
Premelting
+
=
B-enriched, liquid-like
B-enriched, liquid-like
liquid
finite contact angle
 + 
(immiscible)
A
B
Composition
T
Perfect
wetting
Low adsorption
High adsorption
Liquid-like
Crystal
A
B
 is not a stable bulk phase
Liquid is not a stable bulk phase
Plus
additional interfacial forces, e.g., dispersion forces and electrical double-layer forces
Tang, Carter, Cannon, PRL 97, 075502 (2006)
Luo, Tang, Cannon, Carter & Chiang, Mater. Sci. & Eng. A 422, 19 (2006)
Both are “wetting phenomena occurring when the phase that does the wetting is not yet a stable bulk phase.”

## Slide 19: The Sharp Interface Model
Volumetric free energy for forming an undercooled liquid from bulk phases:
vdW London
dispersion
Structural or chemical
Electrostatic
Interfacial forces:
If T < Tsolidus
High-T colloidal forces + a “premelting-like” Gvol term for T < Tsolidus
Analogous to Clarke model for IGFs [J. Am. Ceram. Soc. 70:15 (1987); 76:1201 (1997)]
If h ~ 1 nm
Crystal
Vapor
1 nm
h
Excess film free energy:
for IGFs

## Slide 20
Thermodynamic Principle
h (undercooled liquid)
A subsolidus quasi-liquid film is thermodynamically stable if:
The Excess Free Energy:
Interfacial Interactions
forming
undercooled liquid
solidus
Due to
Short-range
Structural Oscillatory
vdW & Electrostatic (more significant for Ceramic)
Interfacial coefficient
hEQ

## Slide 21: Interfacial Coefficient/Potential
an exponentially-decaying short-range interaction;
a long-range interaction that represents a London dispersion force;
an oscillatory structural interaction leads to layering transitions and produces discrete monolayer, bilayer, trilayer etc. (“hard sphere potential”);
a repulsive short-range force and an attractive long-range force produce an “equilibrium” thickness (indicated by the purple arrow) above the solidus line;
a first-order wetting transition; and
a first-order prewetting transition.
Interfacial coefficient
Interfacial (Derjaguin) Disjoining Potential
= 2cl (rigorously)

## Slide 22
A Phenomenological Thermodynamic Model
The Excess Free Energy:
Interfacial Interactions
Interfacial Coefficient
Combining
Short-range
Long-range
Structural (Oscillatory)
vdW and Electrostatic (Ceramic)
Level I:
Define & quantify:
Omit the details in f(h)
Level II:
Consider f(h) or interfacial(h)
Energetically-Favorite IF:
Multiple Levels of Modeling
Level III:
Diffuse-Interface or Atomistic

## Slide 23:  vs. Film Thickness (heq)
an exponentially-decaying short-range interaction;
a long-range interaction that represents a vdW London dispersion force;
(d), (e), (f) …
Normalizing

## Slide 24: Our Prior Approach – Predictability Demonstrated!
Thermodynamically stable if:
Define & quantify:
Benedictus, Böttger, Mittemeijer, Phys. Rev. 54: 9109 (1996)
A recent review: Jeurgens, Wang, Mittemeijer, Int. J. Mat. Res. 100:1281 (2009)
Co6W7
Bulk
chemical potential
BCC
Liquid
CalPhaD
Miedema type “macroscopic atom” model
(Benedictus-Böttger-Mittemeijer Model)
Representing
the thermodynamic tendency to stabilize a quasi-liquid film
 scales the film thickness
Thermodynamic Functions
(for W-Pd, W-Ni, W-Co, W-Fe): Guillermet, Metall. Trans. A 1989; Gustafson, Metall. Trans. A, 1987; Gustafson, Z. Metallkd. 1988; Gustafson, et al, Z. Metallkd. 1987; Lee et al., Calphad 1986.
Luo & Shi, Appl. Phys. Lett. 92:101901 (2008)

## Slide 25: Applicable to Ni-Bi?
1100 C
700 C
T (K)
Complete Wetting?
(after long annealing, 16 hrs)
Early Argument: No GB complete wetting because vdW is always attractive and longest range force (PRL 1980?)

## Slide 26: Implication
Interfacial Potential
Reducing Bi
 is not film thickness
Minimizing…
In S-L 2-phase region – bilayer stable or metastable?

## Slide 27: Attempt to Construct A Model for Discrete “GB Phases”
Composition
Crystallinity
Orientation
Grain 1
Grain 2
IGF
Excess GB energy:
Excess free energy of the liquid-like GB core (IGF):
Extra interfacial forces:
Volumetric free energy (using standard extrapolation methods in CALPHAD modeling)
Luo, App. Phys. Lett. 95: 071911 (2009)
Tang-Carter-Cannon’s model
PRL 2006
Diffuse-Interface
Lattice-Gas
Lattice-Gas
Introduce an oscillatory force
(in colloidal theories):
(Israelachvili, Intermolecular and Surface Forces, 1994)

## Slide 28
GB “Phase” Diagrams w/ Transition Lines…
However, “ diagrams” appear to be more practically useful at this stage…
In reality, atoms at GBs are more complex than hard spheres (noble gas)!
Grain Boundary Phase Behaviors
“Hard Spheres”
Luo, App. Phys. Lett. 95: 071911 (2009)
Pandit, Schick, Wortis, Phys. Rev. B, 26: 5112 (1982)
Surface Adsorption of
Inert Gas on an Attractive Substrate
Analogous?
Analogous?

## Slide 29: How to Build a Quantitative Model for Ni-Bi and a Model Everything?
Composition can vary layer by layer (but bulk solid prop )
GB phase
different thermo prop.
thickness can vary
Composition can vary layer by layer
Semi-solid, semi-liquid ( vary layer by layer)
Probability of broken bonds (coherency) adjustable
Similar to the Wynblatt-Chatain Model [JMS 2005; 2006, MMA 2007], but assume GB can undergo structural transitions…

## Slide 30: The Bigger Picture – Maybe…
  EA-B - (½EA-A + ½EB-B)
A  |EA |; B  |EB|
Bilayers prevailing?
Negative 
Large Eel
Large A
Small B
Nano-IGFs
dominant?
Classical
L-M
(F-G) 1st-order adsorption transition
  0
Large Eel
Large A - B
Positive  > 2kT
Large XC0 (small Eel)
Multilayer within lattice
Large XC0
Weak segregation (small Eel)
Solid-state prewetting
Premelting
+ prewetting
Ideal case
6 complexions
with 
“Hard wall-hard sphere”
Single 
Network glass
Multiple 
vdW
Solid immiscibility
Small Gamorph
?

## Slide 31: Updates: Experiments on Metal Systems Ni-Bi; Cu-Bi; Fe-Bi Ni-W HRTEM/STEM at Lehigh EBSD/GBCD at CMU

## Slide 32: Ni-Bi, Cu-Bi, and Fe-Bi Samples
Homologous temperature Tanneal/Tmelt = 0.5637
All of the samples were annealed at specific temperatures for 5 hours and quenched immediately in the water.
sample number | system | [M:Bi] powder w/w ratio | Temperature (℃) | hours | Quench methods
20120209001 | Cu-Bi | 0.014:0.986 | 492 | 5 | water
20120209002 |  |  |  |  | 
20120229001 | Cu-Bi | 0.014:0.986 | 492 |  | 
20120229002 | Cu-Bi | 0.014:0.987 | 492 |  | 
20120307001 | Fe-Bi | 0:1 | 746 |  | 
20120307002 | Fe-Bi | 0:1 | 746 |  | 
20120314001 | Fe-Bi | 0:1 | 746 |  | 
20120314002 | Fe-Bi | 0:1 | 746 |  | 
New Samples:

## Slide 33
cleaning boundary
with the presence of
bright “Bi” atoms
clean GB, no evidence
of segregation
EDS point
cleaning boundary
with the presence of
bright “Bi” atoms
TEM-EDX Results of Fe-Bi (Zhiyang Yu)
(lot number 20120307001)

## Slide 34: Hypothesis (Discussed Earlier) – Largely Confirmed
Ni-Bi
Ni-Bi = -14.8 kJ/mol
Cu-Bi = +14.2 kJ/mol
Cu-Bi
Fe-Bi
Cu-Bi = +72.3 kJ/mol
Bilayers ubiquitous
Homologous Temperature Tanneal/Tmelt = 0.5637
A Designed Experiment
Tanneal = 700 C
Tanneal = 492 C
Tanneal = 746 C
Bilayers observed, but in a narrow window
Bilayer NOT observed

## Slide 35: Ni-Bi Samples: Temperature Effects
sample number | system | [Ni:Bi] in Liquid | T(℃) | hours | Quench
20120125001 | Ni-Bi | 0.143:0.857 | 1100 | 5 | water
20120125002 |  |  |  |  | 
20120216001 | Ni-Bi | 0.829:0.171 | 1400 |  | 
20120217001 | Ni-Bi | 0.829:0.171 | 1400 |  | 
20120217002 |  |  |  |  | 
Prior Work: 700 C & 1100 C – virtually identical bilayers
Increase to 1400 C?
Hypothesis: At a higher T, more interfacial disordering?
Moreover, Bi content on the liquidus line drops dramatically above 1300°C
New Samples:
Another Direction (Future): Lower T?
?

## Slide 36: Ziyang’s New STEM on Old Specimens (700 C)
{35-3}
1) Bi adsorption  faceting
2) bilayer formation
(= small S)
Strong Ni-Bi; Weak Bi-Bi
Bi serves as a “surfactant”  “separate” 1 GB to 2 surfaces, each w/ monolayer
Closed-packed surface orientations are stabilized
High-index grain surface  atomic scale faceting
Virtually no relaxation
Some Bi-Bi vdW bonds?
3) CMU: deep groove
Recall CMU earlier results

## Slide 37: Ni-W Electrodeposition Samples Matt Re-started and Prepared a Series of Fresh Specimens
H2O 500mL
NiSO4·6H2O 7.89g (0.06M)
Na3C6H5O7·2H2O 44g (0.3M)
NaBr 7.725g (0.15M)
Na2WO4 · 2H2O 23.25g (0.14M)
NH4Cl 13.25g (0.5M)
Ni film as working electrode
Pt film

## Slide 38: Ni-W Electrodeposition Samples Matt Re-started and Prepared a Series of Fresh Specimens
Ni + ~20 at. %W (starting XRD grain size = ~ 2.5 nm)
Annealed in Ar-5%H2 at 700°C for 4 hrs.
STEM/TEM by Patrick…
Some Fe contamination found (probably from the rust in electrical lead) – Procedure corrected

## Slide 39: Patrick’s STEM – Interesting Microstructure Evolution Upon Annealing at 700 C (4 hrs)
To be further investigated…

## Slide 40
Samples are being prepared to examine effect of annealing conditions on grain growth
  No annealing (as-prepared from electrodeposition)
  700°C for 1 hr.
  700°C for 4 hrs.
    re-prepared to provide sample without Fe and O impurities
  700°C for 24 hrs.
EBSD/GBCD at CMU?
(Proposed future research could include the utilization of pulsed electrodeposition to gain more control over the W doping and surface texture)
Ni-W Electrodeposition Samples

## Slide 41: EBSD/GBCD Specimens for CMU
“Large-area” Ni-Bi and Cu-Bi specimens – (Bi promotes GG Preliminary)
Electrodeposited Ni-W vs. Pure Ni (4-Yr Old Specimens)
Now we can fresh specimens (Replacing)…
Future directions – Controlled annealing experiments in conjunction with Patrick’s work

## Slide 42: Roles of Complexions in Ionic Conduction?
Dr. Matthew Williams and Dr. Jian Luo
Clemson University
MURI Project
Spring 2012

## Slide 43: EIS Setup
One setup can measure EIS on a range of samples from ambient temperature to high temperature range (~1200°C)
supported Pt mesh
Pt wire
Jung, Y.-S., Lee, J.-H., Lee, J.-H., Kim, D.-Y., J. Electrochem. Soc. 150 (2003) J49 – J53.
High frequency data relates to the grain interior while low frequency data relates to the electrodes
The intermediate frequency data is what is directly influenced by the complexions that make up the grain boundaries

## Slide 44: Electrical Impedance Analysis
Through the use of EIS, the contribution from the grain and grain boundaries may be deconvoluted
Babilo, P., Processing and Characterization of Proton Conducting Yttrium Doped Barium Zirconate for Solid Oxide Fuel Cell Applications. dissertation. (2007) Cal Tech.
  Left – intermediate temperature setup in air
  Right – controlled-atmosphere high temperature setup (design in progress)
Planned Research is to understand grain boundary complexion formation and their roles in ion conductivity

## Slide 45: Start Point: SiO2-based Intergranular Films (IGFs) in YSZ – lower O conductivity greatly…
Background & Motivations
Ionic conductors -- important for energy storage & generation.
Many ionic conductors (such as YSZ & BZY) certain GB complexions  severe “blocking effects” to ionic conduction
Additionally, space charges
Guo, X., Waser, R., Progress in Materials Science. 51 (2006) 151 – 210.
Experimental Task II: Roles of Complexions in Ionic Conduction

## Slide 46: GB Transition to Tune Properties Others are already doing this w/o using the concept of GB phase transition
J-H Lee,
Monatsh Chem. 140 (2009)
1081–1094.

## Slide 47: GB Transition to Tune Properties– Via Reducing … Others are already doing this w/o using the concept of GB phase transition
J-H Lee,
Monatsh Chem. 140 (2009)
1081–1094.
(1) To dope the to reduce the chemical potential of SiO2;
or (2) to co-dope (scavenger) or (3) using long pre-sintering annealing to form precipitates
dry IGFs

## Slide 48: Alternative Approach: Conductive IGFs?
Challenge: Glass (or Glass-like IGFs) are usually not good O conductors at all (because O conduction require vacancies).
Attempt in Literature: Using low-melting salts – to form GB conduction “phase”

## Slide 49: How About Proton Conduction?
Enhanced Proton Conduction Demonstarted for LaPO4
Yttria-doped Barium Zirconate (BZY)
Shift to H+-conducting cubic perovskite BZY
  Can function as SOFC electrolyte at intermediate temperature range (500 – 700°C)
  Has similar grain boundary conductivity issues, but much less research has been done
Current research is tackling issues with BZY:
  Ba Stoichiometry
    Tendency to evaporate from structure as volatile BaO at high temperatures
  High Grain Boundary Resistance
    Similar conductivity “blocking” at GBs

## Slide 50: Yttria-doped Barium Zirconate (BZY) Matt Williams
Zr4+ + H2O
Heat to form gel (<150°C)
Calcine ash @ 1250°C / 5hrs.
Stir
Ba2+ + H2O
Y3+ + H2O
Binder burnoff @ 600°C / 30min.
Pelletize w/ binder
Sinter @ 1600°C / 24hrs.
BZY
white powder
Glycine
Heat to ignite (>300°C)
Two methods commonly reported:
  Gel-combustion: very similar to production of YSZ
  Solid-State: stand method used for longest time
Due to potential for weakly agglomerated, smaller particles - GC method examined first

## Slide 51: Synthesis of Yttria-doped Barium Zirconate (BZY) Matt Williams
XRD comparison of interiors of two halves of sintered pellet
From top to bottom – interior of pellet closet to Ba-deficient surface, interior of pellet closest to middle, and calculated pattern from database
Stars mark impurity peaks present due to Ba-deficient phases near exposed surfaces and edges of the pellet

## Slide 52: Another Interesting Idea
To eliminate GBs by column grains in epitaxially grown films
Or, using control AGG to make a single crystal (similar to Al2O3)?

## Slide 53: Backup and Additional Slides

## Slide 55
CMU Experiments on a Second Set of Specimens…
The Effect of Bi on the Surface Morphology of Ni
Ni, 700 °C  15 h in Bi vapor
Ni, 700 °C  15 h (without Bi)
A prior study by Wolski & Laporte [MSEA 495 (2008) 138] showed that annealing in contact with Bi liquid and Bi vapor led to similar GB chemistries (measured by Auger), at least for Cu bicrystals)
Two distinct features:
Bi adsorption  faceting
Some extremely deep grooves
Both can be well explained by the model discussed previously

## Slide 56: CMU Experiments on a Second Set of Specimens … Two Distinct Features – Explained by Our Model
Small!
Ni, 700 °C  15 h in Bi vapor
1) Bi adsorption  faceting
2) Deep grooves
(= small S)
Strong Ni-Bi: ½|ENi-Ni| + ½|EBi-Bi| < |ENi-Bi|
Weak Bi-Bi: |EBi-Bi| << |ENi-Ni|
Bi serves as a “surfactant”
Closed-packed surface orientations are stabilized because they allow more Bi adsorption to reduce   faceting
Binding energy
between 2 Bi layers
Ignore
Anisotropy:
Virtually no relaxation
Some Bi-Bi vdW bonds?

## Slide 57: CMU Experiments on a Second Set of Specimens … Atomic Force Microscopy (AFM)
Measure the width and depth of the grain boundary, infer the dihedral angle and the relative grain boundary energy by the equation
Using the AFM: determine the relative energy of the grain boundaries
D.M. Saylor and G.S. Rohrer, J. Amer. Ceram. Soc. 82 (1999) 1529.

## Slide 58: CMU Experiments on a Second Set of Specimens Measured gb/s
0
.
0
0
.
1
0
.
2
0
.
3
0
.
4
0
.
5
0
.
6
0
.
7
0
.
8
0
.
9
1
.
0
0
.
0
0
.
5
1
.
0
1
.
5
2
.
0
Cumulative Probability
Undoped Ni
Mean = 0.2523
Median = 0.2628
Min = 0.06
Max = 0.71
Bi-doped Ni
Mean = 1.04
Median = 1.08
Min = 0.27
Max = 1.61
gb/s
Ignore anisotropy:
Binding Energy
Virtually no relaxation
Some Bi-Bi vdW bonds?

## Slide 59: Bilayers: Promote or Inhibit Grain Growth (GG)? Some Background & Motivations…
On one hand…
Intrinsic
Bilayer
Monolayer
Trilayer
Nano IGF
Wetting
Dillon, Tang, Carter & Harmer
Acta Mater. 2007
Al2O3
On the other hand…
Stabilization of Nanocrystralline Metals via Doping
Concept/Model:
  Weissmuller (1994)
  Liu & Kirchheim (2002)
Pd-Zr
Fe-Zr
Ni-P:
  Kirchheim et al. (2000)
Ni-W:
  Yamasaki (2000)
  Schuh group (~2007ff)
Ni-Cu
  Pellicer et al., 2011
  Cu-Bi (atomistic modeling)
  Mayr et al.
  Millett et al.
Mayr & Bedorf
PRB 2007

## Slide 60: Stabilization of Nanocrystralline Metals via Doping The Theories
Kinetic Stabilization
Solute drag
Second phase pinning
Chemical ordering
…
Thermodynamic Stabilization (reducing GB to ~ 0?)
competing
The complexion theory argued that segregation induced interfacial disordering can increase GB mobiles (demonstrated in Al2O3, Al-Ga etc.)
A slide from the late
Dr. Rowland Cannon
(2004 GRC)
A GB “phase” transition
(beyond monolayer)?

## Slide 61
Bi Bilayer Adsorption  Significant Reduction of GB (Reducing the Driving Force for Grain Growth)
Average general Ni (“clean”)
Interfacial energy (Ni & Bi-Ni liquid)
Miedema-Type Statistical Models
Experimental: 0.92 J/m2
(700 C, 99.999 wt. % Ni)
But NOT complete wetting because…
(700 C)
Measured average dihedral angle
44.7 (at 700 C)

Bi-Ni Liquid
Decrease to ~1/4 due to bilayer adsorption of Bi
First-principle calculations & atomistic simulations will help to confirm…
Gibbs Isothermal

## Slide 62: Bi Bilayers Appear to Promote Grain Growth (Slightly) Despite a Reduction of the Driving Force (GB) by ~4X
Ni foil
annealed
without Bi
(1100 C, 5 hrs)
Ni foil annealed
in contact with a Bi-Ni liquid
(1100 C, 5 hrs)
Ni foil –
as-received
Verified independently by CMU w/ specimens annealed in Bi vapor (later slides)
Consistent with Dillon and Harmer’s observations/theory for Al2O3.

## Slide 63: On-Going Work… Specimens Prepared at Clemson  EBSD/GBCD Characterization in Progress at CMU
Bi-39 at. % Ni liquid
Ni (free-standing foil, sit on a crucible)
> 2 cm
~2 mm
Annealed at 1100 C, for 5 hrs
in 5 % H2 balanced by Ar
A ridge substrate
Then…
Glue it
Ni foil
Cut the unexposed part
Remove the extra solidified Bi-Ni
Polish off the top layer of ~ 300 m
(initial) grain size: ~75m

## Slide 64: Specimens Prepared at Clemson  HAADF-STEM at Lehigh (Bilayer Observed)  GB Diffusivities Measured at UIUC
bilayer observed by HAADF-STEM
(at this exact GB)
in progress…
Bi-doped Cu (details in the next talk)

## Slide 65: Promote vs. Inhibit Grain Growth? Some More Background …
Ni-W?

## Slide 66: Comparison: Ni-Bi vs. Ni-W
1100 C
Ni
Bi
Ni
W
Miedema Model:
Hmix(50%Ni-50%Bi) = -3.7 kJ/mol
Hmix(50%Ni-50%W) = -4.67 kJ/mol
Low melting;
Strong segregation
High melting;
Weak segregation
Hypothesis?
Inhibit GG?
Promote GG?

## Slide 67: Ni-W: Electrodeposited Specimens Made at Clemson
Thickness : 45 µm
10um
HanSeung Park & Jian Luo
H2O 500mL
NiSO4·6H2O 7.89g (0.06M)
Na3C6H5O7·2H2O 44g (0.3M)
NaBr 7.725g (0.15M)
Na2WO4 · 2H2O 23.25g (0.14M)
NH4Cl 13.25g (0.5M)
  Similar to the Yamasaki (2000) recipe

## Slide 68
Ni-W: Electrodeposited Specimens Made at Clemson
Chart: Na2WO4 · 2H2O (M)
| 0 | 0.14000000000000001 | 0.14000000000000001 | 7.0000000000000034E-2 | 0.21000000000000021
relation | 7.8 | 5.2 | 2.5 | 3.7 | 2.5
Chart: Na2WO4 · 2H2O (M)
| 7.0000000000000034E-2 | 0.14000000000000001 | 0.21000000000000021 | 0 | 0.14000000000000001
 | 15.757 | 22.891 | 21.54 | 6.22
 | 15.443 | 22.179 | 21.09 | 5.91
 | 15.6 | 22.56 | 21.32 | 0 | 6.07
0.3
0.3
S. D.
Chart: at.% W
| 0 | 6.24 | 22.47 | 15.6 | 21.35
 | 7.8 | 5.2 | 2.5 | 3.7
 | at.% W | FWHM | 2-theta | XRD Grain Size
Pure Ni film | 0% | 1.1138 | 44.68 | 7.7nm
0.07M Na2WO4·2H2O | 15.6% | 2.2640 | 43.70 | 3.7nm
0.14M Na2WO4·2H2O | 22.47% | 3.3043 | 44.36 | 2.5nm
0.21M Na2WO4·2H2O | 20.3% | 3.3820 | 44.00 | 2.5nm
HanSeung Park & Jian Luo

## Slide 69: Nanocrystalline Ni + ~20%W – Thermal Stability
 | FWHM | 2-theta | XRD Grain Size
As-deposited | 3.3043 | 44.36 | 2.5nm
400 °C, 6 hrs | 1.4329 | 43.76 | 5.9nm
600 °C, 6 hrs | 0.4330 | 43.62 | 19.7nm
Currently On-Going Tasks
(Preliminary Characterizations)
HAADF-STEM at Lehigh
GBCD at CMU
Worthy to be investigated further?
HanSeung Park & Jian Luo

## Slide 70: Bilayer-to-Trilayer Transition?
A possible GB (Phase) transition?
The transition to a “clean” GB?
Science 2011