## Slide 1: Tailoring of Atomic-Scale Interphase Complexions for Mechanism-Informed Material Design
Atomistic Simulations of Ni-based Systems
Office of Naval Research Multidisciplinary University Research Initiative Project
Review Meeting, Thursday December 15th 2011
ONR Topic Chief: David Shifler

## Slide 2
Classical Atomic Scale Models
Ni-Bi
J. Luo, et al.
Cu-Bi
Ni S3 GB
Widom group
S. Dillon, et al.
Intergranular film in Al2O3
S. Dillon, et al.
Integration

## Slide 3
Atoms are explicitly resolved as point wise masses; interactions between atoms are governed by interatomic potential energy functions, which depend upon the current atomic configuration.
Electrons are not explicitly resolved so computational burden is significantly lower than encountered in quantum mechanical atomic models.
Averaging over (i.e. coarse-graining) electronic degrees of freedom introduces approximations so the validation burden is significantly higher than encountered in quantum mechanical atomic models.
Classical Atomistic Models
Classical Atomic Scale Models
Quantum Mechanical Models
Experiments
For general grain boundaries with large unit cells, we can model structure, thermodynamics, and kinetics with atomic scale resolution.

## Slide 4
Our goal is to explore thermodynamics and kinetics of Bi bilayer complexions observed at GBs in Ni; evidence presented says Bi adsorption on terminating Ni planes is coherent. However, the Bi layer adsorbed on one Ni crystal plane is not coherent with the adjacent grain.
Under what conditions do verified atomic scale models of the same system predict the bilayer structure?
Complexions in Ni-Based Systems
J. Luo, H. Cheng, K. Meshinchi Asl, C. J. Kiely, M. P. Harmer; Science (2011).
For this structure, how does the proposed thermodynamic model correlate with computed GB energy contributions?
What are transport properties of such structures? What are the mechanical properties? How do properties respond to stress and temperature?
How do we learn from these systems to engineer new, complexion based engineered materials?

## Slide 5
Standard pair interaction models (Lennard-Jones) fail to describe metallic systems accurately.
The embedded atom method (EAM) and Finnis-Sinclair (FS) models of atomic interaction were both advanced to overcome this shortfall of pair potentials.
A highly validated EAM Ni model exists; however, no companion model for Bi has been developed (i.e. one needs Ni-Ni, Bi-Bi, and Ni-Bi).
A less-validated, though still quite robust, Finnis-Sinclair model exists for the Ni/Bi system.
Our simulation methodologies and associated characterization tools (post-simulation data processing codes) are generic to the applied model
The tools we’re developing are transferable – not just between models of Ni/Bi but also to atomistic simulations of other systems.
We are utilizing both models – and EAM model of Ni/”Bi” and the FS model of Ni/Bi. Model comparison and further validation will be an integration exercise between the Widom (CMU) and Webb (LU) groups.
Classical Models of Ni/Bi

## Slide 6
The thermodynamic theory that has been advanced to describe Bi bilayer stabilization invokes certain energy relationships that can be explored via atomic scale calculations (both quantum and classical levels of theory).
Atomic Scale Studies of Ni/Bi

## Slide 7
Atomic scale models will evaluate the thermodynamic assertion that complexion stabilization is achieved as a result of minimizing the energy associated with broken bonds at the grain boundary.
Thermodynamic Model

## Slide 8
Determine adsorption properties at free surfaces of Ni as a function of adatom coverage.
Evaluate how adsorption structures change for a model general grain boundary: merge two, rotated free surfaces. How are simple additive rules confirmed and/or challenged.
Compare with more rigorous GB models. Methodology has been advanced for creating low energy GB structures of both tilt and twist types and with varying misorientation/rotation. Such methodology extends to fairly general GBs; however, large unit cells may result.
Classical Model Methodology
S79 symmetric tilt GB in Ni (misorientation q = 33.99°)

## Slide 9
D. Yin (Ph. D. candidate, MSE – LU); combination of electron microscopy and computational techniques to study complexion phases in metallic systems.
Compile massively parallel classical molecular dynamics code LAMMPS.
Determine equilibrium lattice constant of Ni for varying thermodynamics ensembles (a(T)).
Form free crystalline surface simulation ensembles at relevant T (T = 700 °C, 1100 °C; (001), (110), and (111) surfaces).
Compute binding energy and structure of Bi clusters on free surfaces of Ni at “elevated T”.
      energy minimization
      Monte Carlo methods
Build GB structures and repeat dopant adsorption studies.
      high symmetry special boundaries
      low symmetry general boundaries
Graduate Student Update

## Slide 10
Ni is modeled with highly validated EAM potential (i.e. Ni-Ni interactions). For remaining interactions, Bi-Bi is such that the size of the adatom agrees with size of Bi. For interaction strength, EBi-Bi and ENi-Bi are model parameters. Simulations so far fix EBi-Bi and then vary ENi-Bi, with caveat that EBi-Bi < ENi-Bi.
“Bi” on Free Ni Surfaces
Ni (001)
Ni (111)

## Slide 11
Modeling cluster growth (structure, energetics as a function of coverage).
“Bi” on Free Ni Surfaces
Ni (001)
t ≈ 0.1 ms
t ≈ 0.01 ms

## Slide 12
We have almost completed implementing the FS model of Ni-Bi in LAMMPS.
Bi on Free Ni Surfaces
5 at. % Bi and 0.04 at. % Ni (remainder Pb)
Relatively low T compared to our desired state points
Acta Mater. 47 (8) pp. 2477-2484, 1999.
Our model evaluation exercises for free surfaces and GBs are deeply integrated with the Widom group’s optimization exercises.

## Slide 13
Our first studies are using one special boundary (S3) and a small collection of more general GBs (S79, S273).
Bi in Ni GBs
S79 [111] Symmetric Tilt Boundary
(T = 973 K)
View along tilt axis, [1 1 1]
View along normal to tilt axis, [17 -13 -4] / [17 -4 -13]
Creation Methodology: D. L. Olmsted, S. M. Foiles, E. A, Holm; Acta Mater. 57 (2009) 3694–3703

## Slide 14
Our first studies are using one special boundary (S3) and a small collection of more general GBs (S79, S273).
Bi in Ni GBs
S273 [111] Asymmetric Tilt Boundary
(T = 973 K)
View along tilt axis, [1 1 1]
View along normal to tilt axis, [-16 17 -1] / [-19 11 8]

## Slide 15
We are developing a MC based free surface and GB adsorption structure equilibration code.
Establish grand canonical ensembles to permit insertion/deletion of Bi at Ni GB, type swaps between Ni and Bi, and other standard MC structure exploration trial moves
Bi in Ni GBs
View along normal to tilt axis, [-16 17 -1] / [-19 11 8]

## Slide 16
The size ratio of Bi to Cu is quite similar to the size ratio of Pb to Cu; in addition, peculiar surface adsorption behavior has been observed in the Pb/Cu system.
Separate work is investigating adsorption of Pb on Cu(001) and Cu(111) surfaces at elevated temperatures (i.e. T > Tm for Pb).
Some Related Systems
DPb high for overlayer phases … low for surface alloy phases [1]
‘Foot’ diffuses from islands with R ~ t1/2 [2,3]
[1] – J. Moon, et al; Surface Science 488(2001)73-82
[2] – G. Prévot, et al; Phys Rev B 61(2000)10393
Pb
Cu

## Slide 17
Separate work is investigating adsorption of varying size Pb adatom clusters on Cu(001) and Cu(111) surfaces at elevated temperatures (i.e. T > Tm for Pb).
Pb Adatoms on Cu Surfaces

## Slide 18
Separate work is investigating Li transport in graphite GBs to connect with anodic materials for energy storage applications.
Li ‘Dopants’ in Graphite GBs
Pre-addition of Li
Li aggregated at GB on free surface
Li entering GB in graphite

## Slide 19
Converge on an optimized Ni-Bi model.
In parallel with this effort, deploy production ready MC free surface and GB adsorption structure equilibration code.
Compute free surface adsorption structures as well as GB structures for both ‘additive’ GBs and a special (S3) GB in Ni.
Initiate general GB adsorption studies.
Next Six Months (Ni-Bi)