## Slide 1: MURI Program Review, December 2012 Grain Boundary Character Distribution & Abnormal Grain Growth Carnegie Mellon University
Stephanie Bojarski, grad student
William Frazier, grad student
Greg Rohrer
Tony Rollett
Also: Sudipto Mandal, grad student

## Slide 2: Outline
Motivation to Study Complexion Transition Kinetics
Results
  - Relationship between boundary energy and complexion transition nucleation in Alumina
  - Comparison of GBCD between Cu and Bi-Cu - Monte Carlo Modeling of Abnormal Grain Growth (AGG) - 2D - 3D - Hot Pressed Alumina - SPS Alumina - Nano-Ni - 3D Microstructures in Al-Mg for Corrosion Study w/ NRL

## Slide 3: Motivation for Studying Complexion Transition Kinetics and Boundary Populations
COMPLEXIONS:
Are chemically and structurally distinct from the bulk material;
Have their own thermodynamic properties;
Cannot exist in bulk and must exist at an interface;
Like phases, can interconvert between each other;
Typically measured to have lower energy than normal grain boundaries, which is reflected in the relative boundary populations;
Often exhibit exceptionally high boundary mobility, enabling abnormal grain growth to occur.

## Slide 4
Study relations between GB energy and complexion transition nucleation in Alumina
Experimental concept
Low (average) energy grain boundaries
High (average) energy grain boundaries
Al2O3 (hkil)
Al2O3(h’k’I’l’)
Heat, time
Al2O3 (hkil)
Al2O3(h’k’I’l’)
Consolidate samples by SPS
Evaluate average GB energies from thermal grooves
Allow grain growth to occur
Hypothesis is that the complexion transition (marked by larger grains) will nucleate on highest energy GBs

## Slide 5
[010] IPF maps
5μm 10μm
A-Plane:
min: 0.29
max: 1.29
mean: 0.57
median: 0.52
std: 0.23
C-plane:
min: 0.15
max: 1.69
mean: 0.74
median: 0.68
std: 0.35
C
A
500 ppm Y-doped alumina via SPS
Groove 12 hour at 1300°C
MRD
0.80 0.85 0.90 0.95 1.00 1.05 1.10 1.15 1.20
Thermal grooves indicate that the GBs defined by the c-plane have the higher energy
Consistent with GBCD (populations results)
Prediction is that large grains will nucleate on these interfaces
Low pop. High E
High pop. Low E

## Slide 6
500 ppm Y-doped alumina, SPS, anneal 1500 °C for 8h
Groove 12 hour 1300°C
[010] IPF maps
C
A
In this case, observations consistent with the hypothesis!

## Slide 7
Comparison of GB populations in Cu and Bi-Cu
Pure Cu, 900 °C anneal
Cu-Bi, 900 °C anneal
S7 = 38.2 ° around [111]
S3 = 60 ° around [111]
Relatively high energy GBs increase in relative population with Bi adsorption
Lowest energy GBs decrease in relative population with Bi adsorption. Note different intensity scale.
Grain boundary population is useful as a proxy for inverse grain boundary area

## Slide 8
grain boundary relative area, Cu-Bi 900 °C, MRD
grain boundary relative area, Cu 900 °C, MRD
Comparing GBCD of Cu and Cu-Bi
Perfect correlation
S3 GBs, presumably clean, apparent decrease in population due to normalization
GBs which have relatively higher energies in pure Cu appear more frequently in Cu-Bi, implying a reduced energy
Results strongly suggest that Bi complexions in Cu GBs reduce boundary energy and compress the range of energies.
Follow-up: compute the segregation and boundary energy based on EAM potentials and/or 1st principles for a few representative types, e.g. S3 and S5

## Slide 9: Methods for Studying Complexion Transition Kinetics
Examine changes in Grain Size Distribution (GSD) over time.
Examine changes in the size distribution of abnormal grains over time.
Examine AGG as a transformation/recrystallization process that can be described by Johnson-Mehl-Avrami-Kolmogorov (JMAK) kinetic analysis.

## Slide 10: Results: Hot Pressed Ca-Doped Alumina

## Slide 11: Monte Carlo Results – 2D

## Slide 12: 2D Monte Carlo Results – The Extreme Cases Log-Probability Plots of GSDs

## Slide 13: 2D Monte Carlo Results – Continuous vs. Site-Saturated
Continuous, 500 Abnormal spins
Site Saturated, 500 Abnormal Spins

## Slide 14: 2D Monte Carlo Results – AGG Over Time
4*10-4 Nucleations/Pixel
time
time
8*10-6 Nucleations/(Pixel*Step)

## Slide 15: Monte Carlo Results – 3D

## Slide 16: 3D Monte Carlo Models – Continuous vs. Site-Saturated
Continuous Nucleation
Site-Saturated Nucleation
Conclusion: the images do not directly reveal the difference in kinetics

## Slide 17: 3D Monte Carlo Models – Continuous vs. Site-Saturated
.00001 Spins Nucleate/10 Steps
.01 % of 100000 Spins Nucleate
Conclusion: the grain size distributions do not show obvious differences.
This implies that we will need transformation kinetics, i.e. JMAK analysis.

## Slide 18: Experimental Results - Alumina

## Slide 19: Results – SPS Ca-Doped Alumina
Direction: performing experiments to obtain an isothermal annealing series in order to obtain GSDs and JMAK analysis

## Slide 20: Experimental Results – Nano-Ni

## Slide 21: Nano-Ni: Surface Nucleation
Abnormal grains nucleate on the free surfaces of the sample
This explains the trouble obtaining a planar section of abnormal grains
If sample is not mounted flat, then we get a gradient of the surface
Even with surface-linked nucleation, the JMAK exponent should be ~2. Suggests diffusion control of the reaction.

## Slide 22: Nano-Ni: Evolution
Recrystallization-like behavior
Time = t
Time = t + ∆t

## Slide 23: JMAK Analysis of AGG in Nano-Ni
Chart: 
| 8.88183630500415 | 10.26813066612404 | 10.96127784668398 | 11.52089363461941 | 12.75303731591204 | 13.31265310384746
 | -0.90941 | -0.75445 | -0.41376 | -0.0024194 | 0.54527 | 0.95038
ln(time)
ln(-ln(1-X))
JMAK = Johnson-Mehl-Avrami-Kolmogorov Data Adapted From Cheng and Hibbard; similar results for data from by Randle and Coleman
JMAK fit indicates a range of n ~0.5. The value is not consistent with either 2D Site-Saturated (2.0) or Continuous Nucleation (3.0) transformation. It suggests reaction control by fugitive impurity.

## Slide 24: JMAK Analysis of AGG in Nano-Ni
Chart: 
| 2.302585092994046 | 3.401197381662155 | 5.886104031450156 | 6.5792512120101 | 7.090076835776088 | 7.27239839257005 | 7.965545573129986 | 8.88183630500415
 | -2.1988 | -3.3288 | -1.1605 | -0.97971 | -1.293 | -0.98748 | -1.1174 | -0.54196
JMAK = Johnson-Mehl-Avrami-Kolmogorov Data Adapted From Randle and Coleman; similar results for data from by Cheng and Hibbard
JMAK fit indicates a range of n between ~0.25 and ~0.50. This suggests reaction control by fugitive impurity.
ln(time)
ln(-ln(1-X))

## Slide 25
Al-Mg sample from NRL: Pole Figures
CMU previously reported on an analysis of the GBCD, corrected for the moderate texture present in the sample.

## Slide 26: 3D Synthetic Aluminum Microstructure
NRL_5083.ang file used as input
Aluminum (8761 grains)
Ratio of A:B:C is 100:10:1
Sigma spread of Axis ODF s=2
Prebuilt pipeline in Dream.3D used (Synthetic single phases)
Voxel dimensions 100X100X100 used

## Slide 27: Summary
2D modeling of abnormal grain growth suggests measurable differences between continuous and site-saturated nucleation.
3D modeling, however, suggests minimal differences in terms of evolving grain size distributions.
Since the abnormal grains are strongly different in size from the matrix, the evolution is equivalent to recrystallization, therefore we will apply JMAK analysis to Ca-doped alumina.
New series of Ca-doped alumina generated (spark plasma sintered) and annealing started.
AGG occurs in nano-Ni – suggestive of a complexion transition. AGG only occurs near the specimen surface; JMAK analysis suggests dependence on fugitive impurity.
GBCD analysis performed on Al-Mg; also 3D synthetic microstructures built.

## Slide 28: The Size Distributions of Abnormal Grains Over Time
8*10-6 Nucleations/(Pixel*Step)

## Slide 29: The Size Distributions of Abnormal Grains Over Time
4*10-4 Nucleations/Pixel

## Slide 30: 3D Monte Carlo Models – Continuous vs. Site-Saturated
.01 % of 100000 Spins Nucleate