## Slide 1
MURI Program Review
“Tailoring of Atomic-Scale Interphase Complexions for Mechanism-Informed Material Design”
Office of Naval Research, 875 N Randolph Street, Room 603, Arlington, VA 22203
Tuesday, 18 DEC 2012

## Slide 2: Metal Complexionized Ceramics H.M. Chan Dept. Materials Science & Engineering Lehigh University
Goals
Identify complexions with metallic character in alumina
Exploit to form novel materials/property combinations

## Slide 3: Outline
Novel alumina-based systems
1. Al2O3-ITO (indium tin oxide) (Y. Wang)
2. Cu, Ti and Cu-Ti codoped alumina (ppm levels) (A. Lawrence)
Increasing Cu content
Alumina/Cu2O/CuAlO2 (bulk) (M. Kracum)
Decreasing pO2

## Slide 4: Alumina-ITO System
Background
ITO: Composition - 90wt% In2O3, 10wt% SnO2
Melting Point: 1800-2200K
High electrical conductivity ∼104 Ω-1cm-1
cf. (Metal~106-107 Ω-1cm-1)
High optical transparency (>80%)
Composition
Alumina- 10 wt.% (15.8 vol.%) ITO

## Slide 5: Processing: Alumina – 10 wt.% ITO
Starting powders:
alumina powder (AKP-HP, 99.995%, 0.45um)
ITO (Alfa Aesar, 99.99%, 44um)
Processing
Ball milling with ethanol
Dry powder in chemical hood
Press powder before sintering
Sinter powder at 1600oC (1-5 h) air

## Slide 6: In2O3 – SnO2 Phase Diagram

## Slide 7: DC Conductivity –Alumina 10at% ITO (1h, 5h 1600 oC)
For nominally identical processing conditions -
Large variation ( ~ 4000 x) in DC conductivity values!

## Slide 8
High conductivity
Low conductivity
20 mm
2mm
Alumina-15.8vol% ITO
3 distinct phases

## Slide 9
Alumina-15.8vol% ITO
2mm
Al2O3
P
Q

## Slide 10: Phase Relationships
Not consistent with observed microstructures – new phase(s)?
In2O3 – Alumina
Alumina- SnO2

## Slide 11: Alumina-15.8vol% ITO
200 mm
High conductivity
Low conductivity
Microstructures inhomogeneous at macro level
Variation in conductivity due to variations in percolation of conducting phase(s) ?

## Slide 12: DC Conductivity –Alumina 15at% ITO (1h, 1600 oC)
15 at.% ITO

## Slide 13
Compositions: 1000 ppm Cu, 1000 ppm Ti,
600 Cu- 400 Ti, undoped
Processing
Precursors: titanium isopropoxide and copper acetate (in ethanol)
Spark plasma sintering
  Heating and cooling rates of 150 °C/min,
  20 min at 1200 °C, 50 MPa
Grain growth:
Temperature: 1300, 1480, 1750 oC
Time: 1h, 5h, 10h, 20h
Atmosphere (N2-5% H2)
Two different furnaces – Centorr and M60
MCC’s: Low Cu concentrations

## Slide 14: M60 Furnace: Grain Growth
Chart: Grain Size vs. Time: M60
| 1.0 | 5.0
Cu 1300C | 3.478 | 2.795
Cu 1480C | 3.426 | 5.307
Cu 1750C | 5.331 | 5.937
Cu/Ti 1300C | 1.984 | 0.819
Cu/Ti 1480C | 4 | 4.935 | 6.807
Cu/Ti 1750C | 4.452 | 4.202
Ti 1300C | 3.603 | 5.209
Ti 1480C | 5.417 | 8.168 | 10.354
Ti 1750C | 9.506 | 5.689
undoped 1300C | 3.283 | 3.8144
undoped 1480C | 4.619 | 5.3
undoped 1750C | 7.135 | 13.967
Chart: 1000ppm Cu M60
| 0.0 | 0.5 | 1.0 | 1.5 | 2.0 | 2.5 | 3.0 | 3.5 | 4.0 | 4.5 | 5.0 | 5.5 | 6.0 | 6.5 | 7.0 | 7.5
as sps | 0 | 0.072193 | 0.2607 | 0.72861 | 0.94251 | 0.97995 | 0.99465 | 0.99733 | 0.99866 | 0.99866 | 0.99866 | 0.99866 | 0.99866 | 0.99866 | 0.99866 | 1
1300 1h | 0 | 0.040615 | 0.60862 | 0.89969 | 0.97785 | 0.99754 | 1
1300 5h | 0 | 0.043685 | 0.10246 | 0.39237 | 0.7363 | 0.89674 | 0.97379 | 0.99444 | 0.99762 | 0.99921 | 1
1480 1h | 0 | 0.063306 | 0.15826 | 0.43728 | 0.70926 | 0.87104 | 0.95545 | 0.98593 | 0.99766 | 0.99941 | 1
1480 5h | 0 | 0 | 0.083916 | 0.26853 | 0.55385 | 0.82378 | 0.97483 | 0.9972 | 1
1750 1h | 0 | 0 | 0 | 0.18501 | 0.51619 | 0.76133 | 0.89084 | 0.96115 | 0.98612 | 0.99815 | 1
1750 5h | 0 | 0.0053929 | 0.11171 | 0.15716 | 0.25116 | 0.37596 | 0.52388 | 0.66564 | 0.77889 | 0.8698 | 0.92681 | 0.95686 | 0.97843 | 0.99153 | 0.99769 | 0.99769 | 0.99923 | 0.99923 | 0.99923 | 0.99923 | 1
Chart: 600ppm Cu- 400ppm Ti M60
| 0.0 | 0.3 | 0.6 | 0.9 | 1.2 | 1.5 | 1.8 | 2.1 | 2.4 | 2.7 | 3.0 | 3.299999999999999
as SPS | 0 | 0.1794 | 0.63773 | 0.78241 | 0.92477 | 0.96528 | 0.98264 | 0.9919 | 0.99769 | 0.99884 | 0.99884 | 1
1300 1h | 0 | 0 | 0.091408 | 0.44363 | 0.78245 | 0.92931 | 0.9805 | 0.99452 | 0.99817 | 1
1300 5h | 0 | 0 | 0.15729 | 0.60949 | 0.87322 | 0.96271 | 0.9878 | 0.99661 | 1
1480 1h | 0 | 0 | 0.040073 | 0.18852 | 0.43716 | 0.67213 | 0.83698 | 0.9235 | 0.97177 | 0.98907 | 0.99545 | 0.99818 | 1
1480 5h | 0 | 0 | 0.042071 | 0.34385 | 0.72411 | 0.90453 | 0.97896 | 0.99515 | 0.99757 | 1
1480 10h | 0 | 0 | 0.042965 | 0.14743 | 0.40438 | 0.74642 | 0.94103 | 0.98905 | 0.99832 | 1
1750 1h | 0 | 0.0072917 | 0.032292 | 0.18021 | 0.43021 | 0.66979 | 0.84479 | 0.94375 | 0.98229 | 0.99583 | 0.99896 | 0.99896 | 1
1750 5h | 0 | 0 | 0.023585 | 0.059748 | 0.15094 | 0.28459 | 0.40566 | 0.50629 | 0.61321 | 0.7217 | 0.83019 | 0.88679 | 0.91981 | 0.95597 | 0.97956 | 0.99057 | 1
Chart: 1000ppm Ti M60
| 0.0 | 0.4 | 0.8 | 1.2 | 1.6 | 2.0 | 2.4 | 2.8 | 3.2 | 3.6 | 4.0 | 4.399999999999999 | 4.8
as SPS | 0 | 0 | 0.067818 | 0.22072 | 0.4217 | 0.65228 | 0.83477 | 0.92232 | 0.96917 | 0.9815 | 0.99383 | 0.99877 | 1
1300 1h | 0.011968 | 0.36037 | 0.79721 | 0.94747 | 0.98271 | 0.99601 | 1
1300 5h | 0 | 0.00757 | 0.16351 | 0.47464 | 0.74111 | 0.90008 | 0.97502 | 0.99697 | 0.99924 | 1
1480 1h | 0 | 0 | 0.25 | 0.83078 | 0.97364 | 0.9966 | 1
1480 5h | 0 | 0.014479 | 0.070463 | 0.22973 | 0.49807 | 0.76062 | 0.91602 | 0.98166 | 0.99903 | 1
1480 10h | 0 | 0.0017498 | 0.053368 | 0.24934 | 0.5643 | 0.79878 | 0.92913 | 0.97113 | 0.993 | 0.99913 | 1
1750 1h | 0 | 0.011788 | 0.032417 | 0.1277 | 0.26719 | 0.47446 | 0.65521 | 0.80648 | 0.90079 | 0.95285 | 0.99214 | 0.99705 | 0.99804 | 1
1750 5h | 0 | 0.010638 | 0.08156 | 0.29551 | 0.54492 | 0.74113 | 0.86879 | 0.9409 | 0.97281 | 0.98818 | 0.99291 | 0.99764 | 0.99882 | 1

## Slide 15: Grain Boundary Mobilities vs. Temp (M60)
Chart: 1/T (K)
| 0.000635647088736334 | 0.000494315373208107 | 0.000570385580652521
Cu M60 | 5.5755e-16 | 2.3285e-15 | 1.0738e-15
CuTi M60 | 1.9133e-16 | 1.558e-15 | 9.1005e-16
Ti M60 | 8.704e-16 | 6.5915e-15 | 2.2883e-15
un M60 | 9.036e-17 | 5.3315e-16 | 5.7745e-15
Grain growth constant k, calculated and averaged for each temperature group
1750°C
1480°C
1300°C
Decreasing mobility: Ti -> Cu -> Cu-Ti

## Slide 16: Grain Boundary Mobilities vs. Temp
Chart: 1/T (K)
| 0.000635647088736334 | 0.000494315373208107 | 0.000570385580652521
Cu M60 | 5.5755e-16 | 2.3285e-15 | 1.0738e-15
CuTi M60 | 1.9133e-16 | 1.558e-15 | 9.1005e-16
Ti M60 | 8.704e-16 | 6.5915e-15 | 2.2883e-15
Cu Centorr | 2.4069e-17 | 1.2889e-15
CuTi Centorr | 1.5525e-17 | 5.3803e-16
Ti Centorr | 1.0733e-17 | 5.9951e-15
un M60 | 9.036e-17 | 5.3315e-16 | 5.7745e-15
Data falls into two regimes corresponding to furnace
1750°C
1480°C
1300°C
M60
Centorr

## Slide 17: Wetting of Cu on Alumina: Effect of pO2
Enhanced wetting of Cu on alumina at extremes of pO2 values (Saiz et al)
Suggestion that atmosphere in M60 more reducing
Installation of monitor sensitive to very low pO2 values
Saiz, Cannon and Tomsia, Ann. Rev. Mater. Res. 38 (2008) 197-226

## Slide 18: Doped Sapphire Tri-Crystals (Ongoing)
Three alumina single crystals (a, c, r planes) embedded in polycrystalline matrix
  Interfaces immersed in concentrated solution of dopant salt in ethanol
  Sequential process for Ti-Cu co-doping
SPS
Section to expose interfaces
Dope- Ti
Dope- Cu
Anneal- 1300°C 5h
Anneal- 1000°C 5h
SEM/TEM
SEM/TEM

## Slide 19: MCC’s High Metal Concentrations
Approach 1
Alumina + CuO --------> alumina-Cu composite
Target compositions: Al2O3: 0.5, 5, 10 vol.% Cu
Processing
Alumina powder (99.999%)+ CuO (purity 99.995%)
Ball-milled in ethanol for 12 hours
Powder is dried and transferred to a graphite SPS die
CuO reduced in-situ (2 h at 700 oC, 5%H2-95%N2)
SPS 1000 - 1300oC for 25min in the range of 40-60MPa
SPS

## Slide 20: Alumina-0.5 vol % Cu
BSE
5 mm
Cu

## Slide 21
Alumina 5 vol% Cu : reducing atm.
25 mm

## Slide 22
Transition in wetting behavior
25 mm
1 mm
Alumina – “10 vol % Cu”
Cu
At higher wt.% CuO (equivalent to 10 vol% Cu) transition in wetting behavior
Role of trace impurites in graphite foil?
Samples prepared with embedded graphite foil showed no microstructural differences.

## Slide 23
Approach #2
2- step heat-treatment
Alumina-Cu2O starting powders
1. Sinter in oxidizing atmosphere (air)
2. Reduce to Alumina-Cu (Centorr)
- Interest in monolithic CuAlO2
Working Hypothesis
Larger volume fraction of CuO allowed retention of Cu2O and reaction to CuAlO2
Role of CuAlO2
Diemer et al
JACerSoc 82 (1999) 2825-32

## Slide 24: CuAlO2 - delafossite
ABO2 : Stacking sequence of
A+ and BO2 layers
Rhombohedral
Transparent p-type semiconductor
thin films- displays, solar cells
Negative coefficient of expansion
Few studies on bulk CuAlO2
http://www.tcd.ie/Chemistry/staff/people/gww/gw_new/research/TCOs/p-type/
Cu+
Al3+

## Slide 25: Alumina – 21 wt% Cu2O (Air)
Multiple phases present: Cu2O, CuAlO2, Al2O3
CuAlO2 wetting
6h at 1300 oC
5 mm
Al2O3
CuAlO2
Cu2O

## Slide 26
Baldwin et al 1994
Peritectic reaction: L + Al2O3 ---> CuAlO2
5 mm
5 mm
Cored Structure
Alumina-17wt%Cu2O (1300oC for 24hr, air)
Al2O3
CuAlO2
Cu2O

## Slide 27
6h at 1300 oC (air)
5 mm
Al2O3
CuAlO2
Reduction heat-treatment
2CuAlO2 ----- > 2Cu + Al2O3 + ½ O2
Novel alumina-Cu microstructures
5 mm
2 mm
Cu
Al2O3
Reduction
Novel Alumina-Cu Microstructures

## Slide 28
Alumina-17wt%Cu2O (1300oC for 24hr, air)
FIB section from cored region
(C. Marvel, Q. Wu)
2 mm
Al2O3
CuAlO2
CuAlO2
Cu2O
CuAlO2

## Slide 29: Atomic Resolution Microscopy - JEM-ARM200F
Al2O3
Al2O3
CuAlO2
ABF
Boundary inclined- no indication of continuous Cu-rich layer
CuAlO2
Al2O3
CuAlO2
Al2O3

## Slide 30
High Angle Annular Dark Field
HAADF
Fast Fourier Transform
FFT
(3522)
93.6pm
[2201]
Sub-angstrom imaging of the Al2O3 lattice (Z. Yu)
Resolution 0.094 nm (sub- angstrom)!

## Slide 31: Summary and Future Directions
Alumina with Cu (Ti) addition
Strong effect of pO2 on gb behavior at both high and low metal contents regimes
Establish temperature and pO2 regimes that delineate transitions in wetting/microstructure
Installation of ultra low pO2 sensor on M60 furnace
Input from modeling to identify most plausible complexion schemes
Measure electrical and thermal conductivity of Cu/Ti containing aluminas
Fabrication of nano-MCCs by decomposition of CuAlO2
ARM of grain boundaries

## Slide 32: Thank you! Any Questions?