## Slide 1
Simulational Studies of Complexions in the
Ni-Bi System
J. M .Rickman
Materials Science and Engineering and Physics
Lehigh University
E. B. Webb III
Mechanical Engineering and Mechanics
Lehigh University
M. Widom
Dept. of Physics
Carnegie Mellon University
ONR – MURI program
Students
Qin Gao
Denise Yin

## Slide 2
Outline
I. Atomistic Simulation
II. First-Principles Calculations
III Closing the Loop
Finnis-Sinclair potential
semi-grand canonical ensemble
GB composition and structure
segregation and structure
potential development
transport properties (mass and thermal)
- free-standing Bi film
Bi on Ni (111) surface
Bi film in bulk Bi
courtesy J. Luo

## Slide 3
Multiscale Modeling
First-Principles Calculations
Atomistic Simulation
Continuum Description

## Slide 4
Many-Body Interatomic Potential
Landa et al. (1998,1999)
Finnis-Sinclair potential
Cubic spline fit
Ni: 1.24 Angstroms
Bi: 1.56 Angstroms
Atomic Radii

## Slide 5
Methodology
Semi-grand canonical ensemble (Kofke & Glandt, 1987)
Fixed total number of particles
Legendre transforms
T
szz

## Slide 6
1.) S5 Grain Boundary (Ni)
36.90 twist boundary
2.) S13 Grain Boundary (Ni)
22.60 twist boundary
Constructing a Grain Boundary
Bicrystal
S5

## Slide 7
Dm = -1.8 eV
Dm = -2.0 eV
Varying the Chemical Pot. Difference - Layering
S5 bicrystal
z

## Slide 8
Dm = -1.8 eV
Dm = -1.9 eV
radial distribution function
Interfacial Chemistry and Structure
Bi atom

## Slide 9
Segregation Enthalpy
S5 Boundary
DH = 1.25 eV
perform swap (Bi -> Ni) & relax
** Large DH due, in part, to relaxation of elastic energy.

## Slide 10
Impact of Stress
Dm = -1.9 eV
No Stress
Compressive
Uniaxial Stress: 160 MPa

## Slide 11
Bulk alloy phases
Pure Ni surface and grain boundary energies
Bi hcp and hR2 films on bare Ni (111)
Bi atoms and films in pure Ni
First-Principles Studies of Bi in Ni

## Slide 12
Motivation
Quantum size effect of Bi on Ni (111) surface
Experiment:
3,5,7 layer stable films
hexagonal AB stacking (Bollmann etc., PRL, 2011)
Bi Segregation on Ni GB
Experiment:
Bi bilayers at Ni GB’s
(Luo etc., Science, 2011)

## Slide 13
Validation with Bulk Alloy Phases
(Expt.)
(Our Result)
First-Principles Methods
- First-Principles Density Functional Theory Calculations
- Vienna Ab initio simulation package (VASP)
- projector-augmented-wave potentials, PBE generalized - gradient approximation, spin polarization (collinear), relaxed atomic positions and cell parameters

## Slide 14
Bare surface (111):
 = 0.119 eV/Å2
 = 0.149 eV/Å2 (Expt., Tyson, 1977)
Coherent 3 GB (111):
 = 0.028 eV/Å2
 = 0.027 eV/Å2 (Expt., L.Murr, 1975)
Pure Ni Surface and Grain Boundary Energies
3 (111)

## Slide 15: Stability Due to Quantum Confinement
States cross Fermi level periodically
First brillouin zone of bulk hcp (Wiki)
Energy ocillation of freestanding Bi films
Projected band structure of hcp Bi

## Slide 16: Bi hcp films on Ni (111)
[3-112] structure
(3x3) structure
Relative Surface Energy
1ML
1ML

## Slide 17: Stable Bi hR2 films on Ni (111)
1ML

## Slide 18
Bi Films in Bulk Ni
4Ni: B-A-(Bi)-A-C-
5Ni: B-A-(Bi)-B-A-C-
6Ni: B-A-(Bi)-C-B-A-C-
7Ni: B-A-(Bi)-A-C-B-A-C-
Enthalpy of Mixing
ΔH=EBi-Ni - NBiEBibulk - NNiENibulk

## Slide 19
Atomistic Simulation:
Potential Refinement and Transport

## Slide 20
Collaborative efforts at CMU (Widom, et al.) and LU (Webb, et al.) advanced an optimized classical force field for complexion phase systems being studied experimentally.
This effort has continued to more closely investigate the Bi-Bi part of the classical potential.
Review: Optimizing Ni/Bi Model
DFT Classical Classical
(original) (modified)
“Bulk Substitution”
(Ni107Bi) 2.83 eV 4.58 eV 2.83 eV
Bi on Ni(111)
“valley” -4.91 eV -2.94 eV -4.62 eV
Bi on Ni(111)
“bridge” -4.85 eV -2.81 eV -4.48 eV
Bi on Ni(111)
“top” -4.31 eV -2.15 eV -4.01 eV

## Slide 21
Vicinal Surfaces / General GBs
The capability to implement arbitrary (i.e. “general”) GB structures in the classical molecular dynamics simulations has been advanced for the Ni/Bi system.
Experiments
Simulations
The images at left were taken from Luo, et al. wherein they used EBSD to characterize a GB in the Ni/Bi system at which no complexion phase was observed.
For this boundary, experiments reported a 7.5° misorientation from a low index direction perpendicular to [101] (i.e. associated with the vicinal [0 -13 -18] plane).
[0 -13 -18]
The bottom image at left was taken from the same material but shows a GB with pronounced faceting and Bi complexion phase formation.
The image above and at right is from Ni surface simulations en route to preparing models of the experimental GBs at left. Note roughness in the relaxed surface structure).
Depending upon the orientation of the second crystal used to form our bicrystal GB simulation models, we can now form either faceted or low misorientation boundaries.

## Slide 22
Model Predictions – Mass Transport
A goal of the molecular dynamics simulation research is to advance our first predictions about transport properties of complexion phases ahead of corresponding experiments. We will collaborate with Dillon, et al., to ensure predictions made can be tested via experiment.
    Mass transport calculations will reveal diffusivity as a function of complexion phase, grain boundary type (Ni/Bi), and stress.
Webb’s group is already performing mass transport calculations for Bi atoms at model Ni GBs equilibrated by Rickman’s group (S5 GB). We are now embarking on similar calculations for more general GBs.
R(Dt)
(R(Dt))2
4Dt
Diffusivity D2D =
By averaging over trajectories for all Bi atoms in the simulation, we compute a transport quantity that can be compared to experiment.
We will also compute D and grain boundary width d as a function of T; note mass flux scales with the product Dd.

## Slide 23
Model Predictions – Thermal Transport
A goal of the molecular dynamics simulation research is to advance our first predictions about transport properties of complexion phases ahead of corresponding experiments. We will collaborate with Dillon, et al., to ensure predictions made can be tested via experiment.
    Thermal transport calculations will reveal phonon interfacial thermal resistance for varying complexion phases and grain boundary type (Ni/Bi).
Thermal Flux J = GDT = sKDT
If a constant heat flux J is applied across a boundary, a discontinuity in the otherwise linear temperature profile DT will manifest; the magnitude of DT for a given J determines interfacial thermal conductance G or what some call Kapitza conductance sK.
~
~
GB (Periodic)
GB (Periodic)
GB
Heat
In
Heat
Out
100s of nanometers … classical simulations only!

## Slide 24
Thermal Transport Caveat Emptor
Classical MD simulations will reveal the phonon contribution to Kapitza conductace; we will be able to compare sK for clean Ni GBs to complexion phase occupied Ni GBs; we can also compute differences in sK for different complexion phases.
In the absence of modification, classical MD cannot capture the electronic contribution to sK and for the Ni/Bi system, the electronic contribution may be non-trivial.
One possibility is that trends in phononic thermal transport properties will be similar to trends in electronic components of thermal transport; as such, a baseline shift may exist between simulation results and experiment.
Two temperature models exist to rectify the omission of electronic DOFs from classical MD models but these have not been investigated for the Ni/Bi system.
Simulation based predictions made for oxide systems (i.e. clean and complexioned Al2O3 GBs) should robustly compare to corresponding experimental measurements because such systems’ thermal transport properties will be dominated by phonon behavior.
J = sKDT

## Slide 25
Some More on Kapitza Conductance
Bose occupation factor (number of phonons at a given energy and wave vector)
J = sKDT
sK(T) = S ħwlk alk
1
W
dn(wlk,T)
dT
dwlk
dkz
Relevant component of group velocity
Energy transmission coefficient
dn(wlk,T)
dT
dwlk
dkz
alk
Phonon wave packet simulations can be used to compute contributions to sK(T) for different GBs and complexion phases (Schelling et al, Appl. Phys Lett 80, 2484 (2003)).

## Slide 26
Summary and Ongoing Work
1.) Layer Stability
- first-principles results for S1 and Bi on Ni (111)
- layering of Bi at S5 twist boundary
2.) Impact of Stress on Layer Stability
3.) Thermal and Mass Transport
-GB diffusion
- Kapitza resistance and complexions

## Slide 27
Bi Segregation and Layering
S5 GB plane
layer formation
Bi at GB’s
Bi atom

## Slide 28
Stable Bi Films on Ni (111) – from First Principles
Structures
Energetics

## Slide 29
Bi Films in Bulk Ni
Structure
Energetics